i-KRETE MD PRODUCT DATA

Product Description

i-KRETE MD is a four component polyurethane self leveling

system. The standard thickness for i-KRETE MD is a nominal

3-4 mm. Attractive smooth matt colored floor finish.

Uses

i-KRETE MD is formulated specifically for the food and

beverage industry. To provide a good chemical resistance

and hard wearing floor finish i-KRETE MD can be used as a

protective overlay on new floor or to repair floor.

enefits

• Impact resistance.

• Seamless & hygienic finish, no crevices where dirt

and bacteria can dwell.

• Temperature resistant 0℃ to 85℃

• Excellence chemical resistance

• Easy to clean, low maintenance requirement.

• High abrasion resistance

• Low odor during installation

• Smooth surface

Standard Color Chart

Grey          Red          Green

Yellow         Cream

Color matching available with sufficient lead time and minimum order

requirement.

Substrate

i-KRETE MD is suitable for application over concrete, wood,

tile or metal. Not recommended on asphalt o painted

surface.

System Options

Cove Base

To provide for an integral seal at the joint between the floor

and wall. Coving can be formed with i-KRETE Coving Mortar

in conjunction with i-KRETE Primer.

Packaging

i-KRETE MD is packaged in 20 kgs./set, consist of:

Part A and Part B

Part C1 and Part C2 (Easily identifiable Pigment Pack)

Storage & Coverage

Each set of i-KRETE MD will cover approximately as

follow:

• 3.50 sq.m. for thickness 3 mm.

• 2.62 sq.m. for thickness 4 mm.

Substrate preparation

Proper preparation is critical to ensure an adequate

bond. The substrate must be dry and free of grease,

fats, oil and laitance. Totally enclosed shot blasting or

scarification. The surface must be show open textured

surface like a sand paper texture.

Priming

i-KRETE Primer is necessary for applications of i-KRETE

MD over all substrates. The primer system must be cure

to a tack-free state before applying i-KRETE MD

Mixing

• Add Part A and Part B into mixing pail. Mixing

with the blender for 30 seconds.

• Add Part C2 (Pigment Pack) and Part C1 into

mixing pail. Allow the contents to mix until

aggregate is thoroughly “wet out” for 30

seconds.

Pot life

i-KRETE MD has working time of approximately 7 minutes

at 30℃. The working time will vary depending on

temperature.

Application

• Material must be use immediately after mixing.

• Use screed rake to distribute the mixed onto the

floor.

• Use V-notched hand trowel pull the trowel

through the material at right angles to the floor.

• Use a spiked roller to roll the material for allows

air to escape and for the aggregate to be

pushed down allowing liquids to come to

surface.

Hardening Time

At 30℃ allow:

• 8 hours for foot traffic.

• 24 hours for common industrial spillages and

heavy traffic.

Shelf Life

Store unopened in dry conditions at 25-35℃. Avoid

excessive heat and do not freeze. The shelf life is 12

months in original, unopened container.

Cleaning up

Clean up mixing and application equipment immediately

after use. Use toluene or xylene. Observe all fire and

health precautions when handling or storing solvent.

Important

If any unusually long delay should arise, such as a break

for lunch, it will be necessary to completely clean all mixing

paddles and pails before ceasing operation. This is

extremely important. Doing this will prevent the later

contamination of the new batches of i-KRETE MD with

particles of partially cured material when the mixing

operation starts up again after the break. The presence of

such particles would seriously affect the troweling and

finishing of the floor.

Caution

Avoid contact with Part A and B as they may cause skin

and/or eye irritation. In case of contact, immediately flush

area with copious amounts of clean water for at least 15

minutes. Seek medical attention. Applicators should

cover hands with impervious gloves. Wash hands

thoroughly with soap and water after use, and before

eating, smoking, etc.

Physical/chemical characteristics

Compressive Strength 60 N/mm2 after 7 days

(ASTM C-579)

Tensile Strength 15 N/mm2

(ASTM C-307)

Flexural Strength 20 N/mm2

(ASTM C-580)

Hardness 80-84

(ASTM C-2240/Shore D Durometer)

Bond strength > 2.5 MPa

(ASTM C-4541) (100% concrete failure)

Impact resistance >140 in./lbs.

(ASTM C-4226)

Water absorption 0%

(ASTM C-413)

Slip Resistance Dry 70 Wet 25

Pendulum Slip Test

Temperature Resistance:

• 3 mm. -0℃ to 85℃

• 4 mm. -0℃ to 85℃

# Text boxes

i-KRETE MD 產品數據

產品說明

i-KRETE MD是四組份型水性聚胺酯自流平砂漿地坪系統，i-KRETE MD的標準施工厚度是3 - 4 mm，本地坪完成面是美觀的平滑表面。

用途

i-KRETE MD是專門設計使用於食品及飲料產業，可適用於乾燥或潮濕的生產區域地坪，完成後的地坪表面可以抵抗化學品的滲漏噴灑及抵抗磨損。i-KRETE MD不僅可以使用於新建的地坪工程，而且是舊地坪的改修工程的最適當使用材料(快速硬化)。

產品優點

- 耐衝擊。

- 無縫及衛生表面，沒有可供污穢物藏匿及細菌滋生的縫隙。

- 耐溫度抵抗：0 – 85℃。

- 絕佳的耐化學品滲漏噴灑抵抗。

- 容易清潔，低維護需求。

- 高耐磨耗抵抗。

- 施工期間只會產生低臭味。

- 平滑表面。

標準顏色圖表

灰色        棕色        彩綠

黃色        乳黃

特別色需要有較長的訂貨時間及最低訂購量。

基底

i-KRETE MD可施做於混凝土、木質、磁磚或鐵質材料的表面上。不建議施做於柏油或油漆材料的表面上，此類材料必須完全鏟除後才能施做i-KRETE MD。

選用品

圓形衛生踢腳

提供牆面與地坪接縫間的完全密封，可使用i-KRETE Coving Mortar (踢腳用砂漿材料)及i-KRETE Primer (無溶劑型接著密封底塗劑)。

包裝

i-KRETE MD是以小包裝組合方式供應，每組材料包含：

A部(Polyol)、B部(Isocyanate)、C1部(骨料)及C2部(色粉)。

標準用量

每組i-KRETE MD材料大約可施做下列面積：

厚度3 mm：3.50㎡。

厚度4 mm：2.62㎡。

基底表面前處理

適當的基底表面前處理對於確保足夠的接著力是非常重要的

，基底表面必須乾燥而且無油脂、脂肪、油污或其他污染物。

基底表面必須使用噴砂機、刨除機、鑽石磨盤研磨…等方式

預先處理，處理後的基底表面必須有和砂紙一樣的止滑表面。

接著底塗

先均勻塗佈1 mm i-KRETE MD材料(當接著密封底塗劑用)，等接著密封底塗劑表面硬化後才能施做3 mm i-KRETE MD材料。

攪拌混合

- 先將A部及B部倒入攪拌桶內，使用螺旋形攪拌葉片的攪拌機高速攪拌30秒。

- 再將C2部(色粉)及C1部(骨料)倒入攪伴桶內，再高速攪拌30秒，直到骨料完全濕透為止。

材料可施做時間

攪伴後的i-KRETE MD材料硬化時間非常快，可施做時間大約只有7分鐘(30℃)，可施做時間的長短會依施工現場溫度而變動。

應用

- 材料經攪拌後，必須立即施做。

- 使用3 mm鋸齒耙將攪拌後的材料均勻放料於地坪上。

- 使用V型鋸齒狀手鏝刀，將放料的材料修飾到均勻厚度。

- 使用消泡滾筒消除鏝刀及放料耙痕跡，此消泡動作不僅可以將材料內的空氣完全壓出，而且可以將材料內的骨料壓下，使液部材料能夠浮在地坪表面上。

- 詳細施工內容，請參考i-KRETE MD施工說明書。

硬化時間(30℃)

- 完工6小時後可開放步行交通。

- 完工24小時後可抵抗一般工業用化學品的滲漏噴灑及開放重度交通設備。

貯藏期限

將未開封的材料儲存於溫度25-35℃的乾燥場所，避免讓材料過熱或結凍，未開封材料的有效使用壽命為12個月。

設備及工具清潔

完工後立即使用甲苯或二甲苯清潔施工及設備工具，當使用清潔用有機溶劑時，應注意防火及健康的預防。

重要事項

如果預期有長時間中斷施工(例如:午餐休息時間)的情況發生時

，必須清潔所有的施工設備及工具。此清潔動作可以防止先前

施做材料的硬化顆粒污染到後來施做的新材料，此舊材料的硬

化顆粒會嚴重影響i-KRETE MD地坪完成面的品質。

注意事項

避免讓A部及B部的液體材料直接接觸到身體，因為它們可能會引起皮膚或眼睛的敏感。萬一發生此事時，立即用清水沖洗至少15分鐘，如發生皮膚或眼睛敏感時，應立即到醫院接受治療。施工人員應戴上不會透水的橡膠手套，以保護雙手不會接觸到液體材料。施工後、飲食或抽煙前，應先用肥皂及清水清洗雙手。

物理∕化學特性

耐壓強度(ASTM C-579)         ：60 N/mm2 在7天以後

抗拉強度(ASTM C-307)         ：15 N/mm2

彎曲強度(ASTM C-580)         ：20 N/mm2

硬度(ASTM C-2240/Shore D 側硬度器)： 80-84

接合強度(ASTM C-4541)       > 2.5 MPa(100% 混凝土脫落)

衝擊阻力(ASTM C-4226)       >140英吋∕磅。

吸水性 (ASTM C-413)          0%

防滑抵抗(擺錘止滑測試)    乾燥面 70

潮濕面 25

溫度抵抗：

• 3㎜. -0℃~85℃

• 4㎜. -0℃~85℃

廣都工程行  04-25358429   0932-518699    and.and@seed.net.tw     www.a-floor.com.tw